## Slide 1
  Tensys Internal Training
  Derivation of Material Stiffness Properties
  July 2018

## Slide 2: Introduction
Stiffness properties for woven materials, NOT films (ETFE, balloons)
EAw , EAf , EAwf as below, for internal use only.
Use Ew , Ef , nw , nf when reporting to the outside world

## Slide 3: Introduction
Properties determined by biaxial test
Doesn’t have to be fabrication batch
Specialist testing houses
  Dekra, Stuttgart
  Universirty of Essen
  Newcastle University
  Other
Typical sample size is 500 to 700mm2
MSAJ loading protocol and approach

## Slide 4: MSAJ Protocol
Typical loading rate is 2 to 4 mm per minute, e.g. 0.007% per second!
Pre-stress to suit material / Maximum force ~1/4 of tensile strength
Distinct loading regimes, 1:1, 2:1, 1:2, 1:0, 0:1 (5 in total)

## Slide 5: MSAJ Protocol
Standard sheet to plot this out Dekra
Note that loading is relative to pre-stress

## Slide 6: MSAJ Protocol
Alternative loading – tailored towards specific project

## Slide 7: Results
Request raw data excel from testing house, copy into ‘standard sheet’
Typical results – Strain v time

## Slide 8: Results
Typical results – stress v strain
Aim is to define some ‘representative’ properties

## Slide 9: Interrogation
NICK
SEAN
ADAM
ED
Standard sheet for processing of test data
Copy raw test data into standard sheet
Hmmm.

## Slide 10: Interrogation
Aiming to get moduli which match the different parts of the graph
Pick one of the load up curves from each zone

## Slide 11: Interrogation
For one load up identify
  Start warp stress / strain
  End Warp stress / Strain
  Ditto Fill
  Note may be –ve strain
How?
  Interrogate raw tabulated data?
  Hover over graph in excel
  Data entered into processing s/s

## Slide 12: Interrogation
For one load up identify
  Start warp stress / strain
  End Warp stress / Strain
  Ditto Fill
  Note may be –ve strain
How?
  Interrogate raw tabulated data?
  Hover over graph in excel
  Data entered into processing s/s

## Slide 13: Interrogation
Master adjustment tab
Graphical trial and error approach to determine set of representative figures
Overlay of test results in green with stress v strain response calculated from

## Slide 14: Interrogation
Tips
  Ensure graphs have similar strain scales
  If you cant match them all then bias towards expected loading regime
  1:0 F(Ew , Ef) only
  1:2, 2:1 etc F (Ew and n)
  Have a play!

## Slide 15: Interrogation
Final cross check on stress v strain
Both full and zones
Checking both calculated properties AND choice of ‘test’ data against actual test data

## Slide 16: Interrogation
Collate results from different tests
Convert to EA format for inTENS

## Slide 17: Shear stiffness
Shear modulus
Testing undertaken by
  Kawabata, Yokohama University
    Small sample, pre-tensioned and sheared
  Dekra
    Sample at 45 degrees + axial pull
    OR sample at 90 degrees and ‘shear’ pull
  University of Newcastle
    ?
  University of Essen
    ?

## Slide 18: Shear stiffness
Results vary depending on
  Sample pre-stress
  Shear load applied
Further investigation required
Default value is Ew/10